Th = 25.0mm

Tb = 16.0mm

tc = 10. 0 mm

ASME-B31.3

In conclusion: According to Tab-331.1.1 the nominal wall thickness is >13.0mm. Base Metal = P N°4.

So, going to # 331.1.1, Fig. 328.5.4D- sketch (1) the welded joint above doesn’t need to receive PWHT. Is it true?

(BRANCH CONNECTION)

As the welded joint above the thickness through the weld isn’t > 2x the minimum thickness requiring PWHT. Eg;  Tb + tc =  16.0 mm + 10.00 mm = 26.0 mm, that is =  2x the minimum thickness requiring PWHT.