Attachment A

Regarding the mislocated hole repair the AWS code D1.1-2002 outlines one method of repair.  The below figures and comments are created from the commentary of D1.1-2002 Structural Welding- Steel C5.26.5.

“Fill one-half the depth or less with steel backing of the same material specification as the base metal (figure 1).  Then gouge an elongated boat shaped cavity down to the backing (figure 2).  This cavity is then filled by welding using stringer beads. After welding the first side, another elongated boat shaped cavity is made that completely removes the temporary backing on the second side (figure 3).  This cavity is then filled by welding using stringer beads.”

Side views of plate

# Text boxes

Boat shaped gouge 2nd side

Boat shaped gouge 1st side

Steel backing plug

2

3

1