|  | Plate Welding | Pipe Welding | Box Tube Welding |
| --- | --- | --- | --- |
|  | Groove | Groove | Fillet | Butt-Groove | T-,Y-, K-Groove | Fillet | Butt-Groove | T-,Y-, K-Groove | Fillet |
| Thickness Limitations | CJP | PJP |  | CJP | PJP | CJP | PJP |  | CJP | PJP | CJP | PJP |  |
| 1/8" min. | F, H | F, H | F, H | F, H (Note a) | F, H (Note a) | NONE | F, H (Note a) (Note c) | F, H | F, H (Note b) | F, H | NONE | F, H (Note c) | F, H (Note c) |

| NOTES |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| a: Only qualified for pipe 24 inches in diameter or larger with backing, backgouging or both. |  |  |  |
| b: Not qualified for joints welded from one side without backing, or welded from two sides without backgouging |
| c: The dihedral angle for T-, Y-, K- Groove is 30° minimum |  |  |  |  |  |  |